ELECTROCHEMICAL PROPERTIES OF 2,6-BIS((E)-2-(FURAN-2-YL) VINYL)-4-(AZULEN-1-YL) PYRIDINE

# Oana Iulia ENACHE1, Ovidiu-Teodor MATICA1, Magdalena-Rodica BUJDUVEANU1,

# Raluca ISOPESCU1, Mihaela CRISTEA2, Eleonora-Mihaela UNGUREANU3

## 1Faculty of Chemical Engineering and Biotechnologies, University POLITEHNICA of Bucharest, Romania

## 2Institute of Organic Chemistry C. D. Nenitzescu of Romanian Academy, 202B Spl. Independentei, 71141, Bucharest, Romania

## 3Doctoral School “Appllied Chemistry and Materials Science”, University POLITEHNICA of Bucharest, Romania

## oana.enache18@yahoo.com / em_ungureanu2000@yahoo.com

Background:  Azulene derivatives were investigated by electrochemical methods to establish their ability to recognize heavy metal (HM) ions for analytical purposes, such as sensors. 4-(azulen-1-yl)-2,6-bis((E)-2-(furan-2-yl)vinyl)pyridine (L) ligand was previously synthetized and characterized by physical chemical methods.

Aim: Starting from this premise, the present study focused on the investigation of L, to evaluate its sensory response for HM ions.

Method: The electrochemical study of L was performed on glassy carbon working electrode by using cyclic voltammetry (CV), differential pulse voltammetry (DPV), and rotating disk electrode voltammetry (RDE). Polymeric films were formed by electrochemical oxidation either by cycling the potential in the anodic scans or by controlled potential electrolysis at different anodic potentials and charges. The obtained modified electrodes were tested as sensors for heavy metal ions

Results and discussion: The formation of thin films is confirmed by the comparative recorded cathodic CV curves in ferrocene (Fc) solution of the obtained L-CMEs and of the bare electrode.

Stripping peaks for Cd, Pb, Cu and Hg ions (each having a 10-5 M concentration) were noticed at different potentials. For each investigated HM ion, the DPV curves in the tested accumulation solutions showed the corresponding stripping peak currents which are higher than for bare electrode indicating that these ions have been retained in the electrogenerated films, ensuring the immobilization into L complexing units in different percentages.

Conclusion: One of the results shows that the estimated detection limit of Pb species is less than 10-8 M.

Acknowledgments

This research was funded by Romanian National Authority for Scientific Research, UEFISCDI, under grant PN-III-P2-2.1-PED-2019-0730, contract no. 293PED/2020.

Keywords: 2,6-bis((E)-2-(furan-2-yl) vinyl)-4-(azulen-1-yl) pyridine, voltametric methods, chemically modified electrodes, heavy metal ions detection