influence of mg and zn content on the properties of hydroxyapatite based coatings

# D.M. Vranceanu1*, I.C. Ionescu1, E. Ungureanu1, A. Kiss2,

# A.C. Parau2 and C.M. Cotrut1

1- University POLITEHNICA of Bucharest, 313 Independeței Street, Bucharest, Romania

2- National Institute for Optoelectronics, 409 Atomistilor Street, Magurele, Bucharest, Romania

## diana.vranceanu@upb.ro

Background: Biomaterials are an integrated part of modern medicine, and their development and improvement are essential.

Aim: Thus, the aim of this research was to obtain hydroxyapatite (HAp) based coatings doped with different concentration of Mg (H/MgX, where X is 1 and 1.5 mM of Mg(NO3)2·6H2O in the electrolyte) and Zn (H/ZnY, where Y is 0.015 and 0.020 mM of Zn(NO3)2·6H2O in the electrolyte) on Ti nanostructured surface through electrochemical techniques, and to evaluate the influence of the doping elements content on the physico-chemical properties of HAp. All electrolytes were prepared with respect to (Ca+M)/P ratio of 1.67, where M is Mg or Zn concentration.

Method: The HAp based coating were electrochemically deposited in galvanostatic pulsed mode on titania nanotubes. The materials were analysed by SEM-EDS, XRD and FTIR. The coatings adhesion on the substrate was also investigated.

Results and discussion: All coatings present a morphology that consists in ribbon like crystals. XRD and FTIR have confirmed the formation of HAp phase in all coatings. Addition of the doping elements in smaller amounts don’t alter the coatings adhesion.

Conclusion: The results have indicated that addition of Zn or Mg in smaller amounts enhances the properties of HAp coatings, compared to higher ones.

Acknowledgments: This research has been funded by the Romanian Ministry of Education and Research, CNCS - UEFISCDI, project number PN-III-P1-1.1-TE-2019-1331, within PNCDI III (project no. TE 172/2020; 3B-CoatED).

Keywords: hydroxyapatite; coatings; electrochemical deposition.