BIOPOLYMERIC COMPOUNDS WITH MEDICINAL APPLICATIONS

Dana-Maria Miu1,2, Ramona-Daniela Pavaloiu1, Gabriela Savoiu1, Maria Spiridon1, Mihaela-Carmen Eremia1

## 1The National Institute for Chemical Pharmaceutical Research & Development, 112, Vitan Ave 031299, district 3, Bucharest, Romania

2Faculty of Chemical Engineering and Biotechnologies, 1-7 Gheoghe Polizu st., sector 1, 011061, Bucharest, Romania
e-mail address: dana.miu92@gmail.com

Background: Biopolymers derived from nature sources or microbial have grown in importance in the medical field. They are used alone or in polymeric complexes, in tissue engineering for tissue reconstruction, or as drug delivery systems in combination with drugs to accelerate regeneration. Among the various biomaterials available for therapeutic applications, polyhydroxyalkanoates (PHAs) offer new properties as biomaterials of interest due to their high biocompatibility, as well as their biodegradability and various thermo-mechanical properties.

Aim: This paper takes into account the leading medical representatives of biopolymers with medical applications (PHAs and polysaccharides), with a particular focus on obtaining a scaffold hybrid biomaterial composed of biopolymers (e.g., polyhydroxybutirate and chitosan) and bioceramic material.

Method: To create the hybrid biomaterial, each biopolymer was dissolved in a trifloroacetic solution at a temperature of 35-40°C. After thoroughly mixing the two polymeric components, the bioceramic was added and stirred for approximately one hour at 45°C. The mixture was poured into a Petri dish and left to evaporate overnight.

Results and discussion: Following the trials, distinct flexible and translucent films, easily processed for medical purposes, were obtained depending on the ratio of the component polymers.

Conclusion: Although only PHB has been approved by the FDA for medical applications, its demonstrated favorable properties (immunologically inert, biocompatible, rapid tissue growth, bioresorbable, slow biodegradable tissue scaffolds), as well as a large number of promising studies with other PHAs, indicate an optimistic outlook for the development of those biopolymers alongside natural biopolymers.

Keywords: polyhydroxyalkanoates, polysaccharides, bioceramics, scaffolds

Acknowledgments: This work was supported by a grant of the Ministry of Research and Innovation, project number PN-19-410401 (Contract 34 N/2019).